- Crystal Lattice Energy (U0):

The energy change when a mole of solid crystal is formed from its constituent ions in their gaseous state.

How To Calculate Crystal Lattice Energy

Crystal lattice energy (U0) can be calculated using Born-Lande equation:

U0 = (A NA z+ z− e2 /4 π ε0 r0) (1–1/n)

- A is the Madelung constant, relating to the geometry of the crystal;

- NA is the Avogadro constant;

- z+ is the charge number of positive ion;

- z− is the charge number of negative ion;

- e is the electronic charge, equal to 1.6022×10−19 C;

- ε0 is the permittivity of free space, equal to 8.854×10−12 C2 J−1 m−1;

- r0 is the distance to closest ion;

- and n is the Born exponent, a number between 5 and 12, determined experimentally by measuring the compressibility of the solid, or derived theoretically.